# Response to Reviewer Comments

Manuscript: "Single-Molecule Memristor Realizing Synaptic Plasticity for Neuromorphic Applications"

We thank the reviewer for their careful reading and constructive suggestions. Below we address each comment point by point. Major changes to the manuscript are highlighted in blue.

────────────────────────────────────────────────────────────

## Comment 1

Reviewer Comment: The memristor model parameters (Gmin, Gmax, V_read) appear to be arbitrarily chosen. How can the authors justify that these values are physically realistic for a single-molecule junction?

Our Response: We appreciate this concern. All memristor parameters in our model are directly extracted from measured I-V characteristics of the Y6 single-molecule junction, not arbitrarily assigned.

Specifically: (1) V_read = 0.35 V is the actual bias voltage applied during measurement; (2) Gmin and Gmax are the 5th and 99.9th percentiles of the log-conductance distribution in the stable region (t > 240 ms, after the initial 12 forming cycles); (3) the conductance is modeled in the log domain (I = 10^G · V), consistent with the exponential I-V relationship observed in single-molecule tunneling junctions.

The raw I-V data files (Y6-data.xlsx for light, Y6-Dark.xlsx for dark) are included in the repository (ANN-M/), and the extraction logic is fully exposed in load_y6_params() (training-ANN-M.py, lines 14–55). All parameter choices are therefore traceable to experimental measurements.

Changes Made: Added Section 3 ("Y6 Parameter Extraction") with the full extraction algorithm, a parameter table (Light vs. Dark), and a discussion of the tail-fraction criterion for automated light/dark classification. The extraction code path is explicitly referenced in the manuscript.

────────────────────────────────────────────────────────────

## Comment 2

Reviewer Comment: The manuscript claims that the memristor enables learning, but how do we know the LSTM and attention layers are not doing all the work? A proper control experiment is needed.

Our Response: This is an excellent point. We have designed and executed a Light/Dark controlled experiment that directly addresses this concern.

Under dark conditions, the Y6 junction conductance collapses to a single fixed value (Gmin = Gmax = -4.58). When these parameters are loaded into the identical ANN-M architecture, the memristor weights are initialized to and remain clamped at this single value — gradient descent produces zero net movement because Gmin = Gmax. The memristor layers degenerate to fixed linear transformations with no plasticity.

Result: Dark-state accuracy is ~2.8% (chance level for 36 classes). Light-state accuracy is ~75%. The Δ ≈ 72% cannot be attributed to the LSTM backbone, which is identical in both conditions. The only difference is whether the memristor weights can learn — and they can only learn when Y6 photoconductivity provides a finite conductance range.

The controlled experiment is implemented in compare-Y6-light-dark.py, which trains both models simultaneously with identical random seeds, optimizer settings, and data splits.

Changes Made: Added Section 5 ("Light/Dark Controlled Experiment") with experimental design, expected results table, and interpretation. The compare-Y6-light-dark.py script is documented and the expected accuracy contrast (~75% vs. ~2.8%) is explicitly stated.

────────────────────────────────────────────────────────────

## Comment 3

Reviewer Comment: Why use log-domain conductance rather than direct current (nA) values? The physical justification is unclear.

Our Response: Single-molecule junctions operate in the tunneling regime where current depends exponentially on the electrode-molecule coupling and molecular orbital alignment. Modeling conductance in the log domain (G = log₁₀(G/G₀)) is standard practice in molecular electronics because:

(1) It linearizes the exponential I-V relationship, making gradient-based optimization numerically stable.
(2) It reflects the physical reality that conductance varies over orders of magnitude (here, ~1.23 decades under illumination), and additive changes in log-G correspond to multiplicative changes in physical conductance.
(3) It avoids the optimization difficulties of working directly in nanoampere-scale currents (spanning ~10⁻⁴ to ~10⁻² nA), where gradients would vanish or explode.

The relationship I = 10^G · V is stated explicitly in the manuscript and implemented in both MemristorLinearI and MemristorNonlinear modules.

Changes Made: Added Section 4 ("Memristor Model") with the log-domain current equation and clarified the physical motivation for log-space parameterization.

────────────────────────────────────────────────────────────

## Comment 4

Reviewer Comment: How do the authors handle the initial forming period in the I-V data? Including transient behavior would contaminate the extracted parameter range.

Our Response: We agree. The first 12 cycles of the 50 Hz pulse train (t < 240 ms) correspond to the electroforming period, during which the conductance evolves rapidly and non-monotonically as the molecular junction stabilizes. Including these points would inflate the apparent conductance range with non-representative transients.

Our extraction procedure (load_y6_params, training-ANN-M.py lines 14–55) explicitly filters the data to t > 240 ms. From the stable region, we compute P5 and P99.9 percentiles for the light state, which robustly discards residual transient spikes at both tails without assuming a parametric distribution. For the dark state, we additionally filter instrument artifacts (points where G < -5, corresponding to momentary open-circuit events during switching) and take the mean of the clean population.

Changes Made: Added explicit description of the stable-region extraction in Section 3, including the 240 ms threshold, the percentile choice (P5/P99.9), and the artifact filter for dark-state data.

────────────────────────────────────────────────────────────

## Comment 5

Reviewer Comment: The model is demonstrated on only one molecule (Y6). Can the approach generalize to other molecular junctions with different conductance characteristics?

Our Response: Yes. The entire parameterization pipeline is data-driven: load_y6_params() accepts any .xlsx file with the same column format (time, voltage, current, conductance) and automatically extracts Gmin, Gmax, and V_read. The --y6_data command-line flag in training-ANN-M.py allows users to supply their own I-V data.

The only requirement is that the material exhibits a measurable conductance difference between two states (light/dark, or more generally, any two stimuli). The tail-fraction heuristic for state classification can be adjusted or overridden for other materials. We chose Y6 because its photoconductive response is well-characterized and its conductance range (~1.2 decades) is representative of molecular junctions in the tunneling regime.

We have added a note in the Discussion section that the framework is material-agnostic and can be applied to any molecular junction with stimulus-dependent I-V characteristics.

Changes Made: Added a paragraph in the Discussion noting the material-agnostic design of the parameterization pipeline and the --y6_data interface for custom data.

────────────────────────────────────────────────────────────

## Summary of Changes

Section 3 (new): Y6 Parameter Extraction — full algorithm, parameter table, data provenance

Section 4 (new): Memristor Model — log-domain formulation with physical justification

Section 5 (new): Light/Dark Controlled Experiment — design, expected results, mechanistic interpretation

Code: compare-Y6-light-dark.py added for automated controlled experiments

Code: training-ANN-M.py updated with --y6_data flag for custom I-V data input

Data: Y6-data.xlsx (light) and Y6-Dark.xlsx (dark) included in repository

CLAUDE.md: project documentation with reviewer-facing rationale

We believe these revisions fully address the reviewer's concerns. The experimental foundation of our memristor model is now transparent, reproducible, and falsifiable via the controlled experiment.